SELF ADHESIVE SHEET PERMEABLE AIR BARRIER

SOPRASEAL STICK VP

FOR A COMPLETE DESCRIPTION OF PRODUCTS AND APPLICABLE STANDARDS, PLEASE REFER TO THE TECHNICAL DATA SHEETS (SOPREMA SPECIFICATIONS MANUAL OR WEB SITE WWW.SOPREMA.CA).

PLEASE CONTACT A SOPREMA REPRESENTATIVE TO ASSIST IN THE DESIGN OF SPECIFICATIONS FOR A PARTICULAR PROJECT.

THE ELECTRONIC VERSION OF SOPREMA’S SPECS IS AVAILABLE ON OUR WEB SITE: WWW.SOPREMA.CA.

# GENERAL

## DESCRIPTION

### This section specifies the requirements for the supply and installation of the elements required for vapour permeable air barrier membrane.

### Vapour permeable air barrier system: Self-adhesive tri-layer laminated polypropylene facer.

## RELATED WORK

### Division [02 40 00] [Demolition and Structure Moving]

### Division [03 00 00] [Concrete]

### Division  [04 00 00] [Masonry]

### Division [07 10 00] [Dampproofing and Waterproofing]

### Division [07 21 00] [Thermal Insulation]

### Division [07 50 00] [Membrane Roofing]

### Division [07 84 00] [Firestopping]

### Division [08 10 00] [Doors and Frames]

### Division [08 50 00] [Windows]

### Division [09 29 00] [Gypsum Board]

### Others	[              ] [              ]

## COMPLEMENTARY WORK TO BE EXECUTED BY THE SUB-CONTRACTOR

## TECHNICAL DOCUMENTS

### Submit two (2) copies of the most current technical data sheets. These documents must describe the physical properties of the material, and explanations about product installation, including installation techniques, restrictions, limitations and other manufacturer recommendations.]

## CONTRACTOR QUALIFICATIONS

### Vapour permeable air barrier work shall be performed only by skilled applicators, employed by an installation contractor operating all adequate and necessary equipment to execute such work in accordance with the manufacturer’s recommendations and recognised standards.

## MANUFACTURER'S REPRESENTATIVE

### The vapour permeable air barrier materials manufacturer may delegate a representative to visit the work site at commencement of work.

### At all times, the contractor shall permit and facilitate access to the site by the manufacturer's representative cited above.

## MATERIALS STORAGE

### Handle rolls of materials with care and proper equipment.

### Rolls of materials shall be carefully stored and adequately protected in accordance with the manufacturer’s recommendations.

## QUALITY ASSURANCE AND ENVIRONMENTAL MANAGEMENT

### The manufacturer of permeable air barrier products will provide proof of ISO 9001 and ISO 14001 Certifications.

## WARRANTIES

### The product manufacturer shall issue a written and signed document in the name of the owner, certifying the product will meet all the physical characteristic published by the manufacturer, for a period of 5 years, starting from the date of completion of installation of membranes. No letter amending the manufacturer’s standard warranty will be accepted and the warranty certificate must reflect these requirements.

# PRODUCTS

## VAPOUR PERMEABLE AIR BARRIER MEMBRANE

### Description: Membrane composed of a tri-layer laminated polypropylene facer. The self-adhesive underface is covered with a silicone release film; for use in wall construction as primary air barrier material, through wall flashing and membrane transition.

### Components:

#### Surface:	Tri-Laminate Polypropylene.

### Properties:

#### Thickness:	0.6 mm (24 mil)

#### Tensile strength (kN/m):	(MD) = 5.95 - (XD) = 3.65

#### Tear resistance (N):	(MD) = 64 - (XD) = 54

#### Water vapour permeability ASTM E96-B (perm): 8.7

#### ASTM E96-A (perm): 7.6

#### Cold bending at – 30°C (-22°F): No cracking

#### Dimensional stability at 85°C (185°F): (MD) = -0.45 - (XD) = 0.11%

#### Plywood adhesion:	356 N/m

#### Lap joint strength:	300 N/m

#### Adhesion after elevated temperature exposure AAMA 711-05, level 3, 7 days @ 80°C (176°F): 1200 N/m

#### Air permeability 75 Pa (L/sec* m²):	0.0025

#### Nail sealability: Pass

### Specified products: SOPRASEAL STICK VP by SOPREMA.

## PRIMER FOR SELF-ADHESIVE MEMBRANES

### Description:  A water-base polymeric primer that contain no bitumen which is  used to enhance adhesion of self-adhesive membranes on most surfaces.

### Specified product: ELASTOCOL STICK H2O by SOPREMA.

## ACCESSORIES

Note:	Install a self-adhesive membrane strip beneath upstands and parapets and at wall junctions to ensure air / vapour barrier continuity, as specified below. For on-site co-ordination, this membrane must be provided by the roofer and installed by a carpenter. Specify the installation of this strip in the Carpentry Section.

### ROOF TO WALL TRANSITION MEMBRANE

#### Specified products: SOPRASEAL STICK 1100 T by SOPREMA

### WATERPROOFING SEALANT

#### Description:  A moisture cure, silylated polymer elastomeric sealant.

#### Specified product:  SOPRASEAL SEALANT by SOPREMA.

Note:* Cut rolls are available upon request for all tapes around windows.

### TAPES AROUND WINDOWS

#### Specified product: SOPRASEAL STICK 1100 T in pre-cut rolls by SOPREMA.

#### [OR]

#### Description:  Multi-purpose self-adhesive membrane composed of SBS modified bitumen, self-protected by an aluminium sheet.

#### Specified product:  SOPRASOLIN HD by SOPREMA.

### THROUGH-WALL MEMBRANE

#### Specified product: SOPRASEAL STICK VP by SOPREMA.

#### [OR]

#### Description:  Self-adhesive membrane composed of SBS modified bitumen and a strong Tri-Laminate Woven Polyethylene facer.  The self-adhesive underface is covered with a silicone release sheet.

#### Specified product:  SOPRASEAL WFM by SOPREMA.

# EXECUTION

## EXAMINATION AND PREPARATION OF SURFACES

### Surface examination and preparation must be completed in conformance with recommendations in the SOPREMA Specifications Manual.

### Before waterproofing work begins, the owner's representative and the membrane contractor’s foreman will inspect and approve substrate condition and ensure that related work has been properly executed. If necessary, a non-conformity notice will be issued to the contractor so that required corrections can be made. The start of the membrane application will mean that substrate conditions are acceptable for work completion.

### Before commencing work, all surfaces must be smooth, dry, clean and free of ice and debris as per manufacturer’s recommendations.

### No materials will be installed during rain or snowfall.

### Concrete must be cured a minimum of fourteen (14) days and an adhesion test is recommended before membrane application.

### Any gap larger than 6.4 mm (1/4 inch) needs solid backing. The gap should be filled in.

### At deflection joints, a 150 mm (6 in.) wide reinforcement strip of self-adhesive membrane centered on the joints should be installed.

## METHOD OF EXECUTION

### Work shall be performed on a continuous basis as surface and weather conditions allow.

### Adjoining surfaces shall be protected against any damage that could result from the waterproofing installation.

## EQUIPMENT

### Maintain all equipment and tools in good working order.

## PRIMER APPLICATION

### Surface where primer is required (specific site conditions) shall receive polymer emulsion-based primer coating at the rate of 0.1 to 0.3 L/m2. Primed surfaces must be covered the same day.  If not covered the same day, primed surfaces must be re-primed.

## VAPOUR PERMEABLE AIR BARRIER MEMBRANE INSTALLATION

### All inside corners should be covered with a 150 mm (6 in) wide strip of membrane centered on the corner. This membrane must be installed in direct contact with the substrate not leaving any voids under the membrane.

### Install the membrane on the surface by peeling back the release film on the underside and adhering the membrane to the surface.

### Side lap joints must be a minimum of 50 mm (2 in) and end lap joints must be minimum of 75 mm (3 in).

### Holes and tears in the membrane must be repaired with vapour permeable air barrier membrane material.  The repair must exceed the affected surface area by a minimum of 100 mm (4 in).  The membrane piece applied for the repair must be sealed around its edges with waterproofing sealant.

### Use a roller recommended by the manufacturer to apply pressure over the entire surface of the membrane to ensure uniform adhesion to substrate.

### The contractor shall inspect membrane installation meticulously at the end of each day of work and also before installation of insulation.  The upper edge of the membrane must be sealed with waterproofing sealant at the end of the day's work when precipitation is anticipated or when the work is expected to be delayed or interrupted by more than one day.

### All small protrusions (pipes, etc.) through the waterproofing membrane, should be pre-stripped with a membrane and sealed with waterproofing sealant.

### Insulation or covering material should be installed as soon as possible following inspection of the membrane by a professional (maximum exposure 180 days).

## THROUGH-WALL FLASHING MEMBRANE INSTALLATION

### Through-wall flashing membrane should be installed where applicable, as indicated on drawings.

## MEMBRANE INSTALLATION AT OPENINGS (Windows, doors, etc.)

### The membrane must be carefully installed around openings in the wall (windows, doors, etc.) in such a manner as to prevent any air leak at these areas (refer to drawings for details).  The vapour permeable air barrier membrane must be installed to create a continuous seal at construction elements such as foundations, roofs and walls, and at junctions of different materials or construction types (curtain wall construction, etc.).

### Self-adhesive membranes applied to junctions, window frames, door frames, endings, and on the perimeter of the building, receiving a sprayed insulation, should be mechanically fastened to the substrate with a termination bar.

Note: 	SOPREMA INC. may modify the composition and/or utilisation of its products without prior notice.  Consequently, orders will be filled according to the latest specifications.

-END OF SECTION-