THERMAL INSULATION

SECTION 07 21 19

Foamed-in-Place Insulation

HEATLOK® HFO High Lift

Display hidden notes to specifier by using “Tools”/”Options”/“View”/”Hidden Text”.

For later versions of Word, use “Office Button”/”Word Options”/”Display”/Hidden Text”.

.3.** NOTE TO SPECIFIER ** DEMILEC®; spray foam thermal insulation.

.

This section is based on the products of DEMILEC®, which is located at:

3315 East Division Street,

Arlington, TX 76011

Toll Free Tel: (888) 224-1533

Tel: (817) 640-4900

Fax: (817) 633-2000

Email: buildingscience@demilec.com

Web: http://www.demilec.com

Since its inception in 1997, DEMILEC® has served as the American presence of DEMILEC, Inc., a Canadian manufacturer and distributor of polyurethane and Polyurea products and systems.

From our 40,000-square-foot manufacturing facility @ 2925 Galleria to our state of the art 223,700-square-foot corporate center in Arlington, Texas @ 3315 East Division St., DEMILEC has become an industry leader in developing a variety of polyurethane foam insulation products for residential and commercial construction. To complement our insulation products, DEMILEC has developed superior services and partnership programs for contractors and builders throughout the United States and in seven foreign countries. These services and programs range from product application training to developing next-generation financial packages that make energy-smart homes more affordable.

Now in our second decade, DEMILEC has become an industry pioneer in the field of high-performance polyurethane and Polyurea products. As the importance of environmentally friendly products has grown, we have dedicated our company to developing environmentally friendly spray foam insulation products that are setting new standards for affordability, performance and energy efficiency in commercial and residential construction.

.

GENERAL

SECTION INCLUDES

** NOTE TO SPECIFIER **  Delete items below not required for project.

Spray-in-place rigid (closed cell, 2 pound foam) polyurethane foam insulation in various assemblies, to provide an air barrier and improved thermal resistance.

RELATED SECTIONS

** NOTE TO SPECIFIER **  Delete any sections below not relevant to this project; add others as required.

Section 03300 - Cast in Place Concrete.

Section 03400 - Structural Pre-cast Concrete.

Section 04200 - Unit Masonry.

Section 05300 - Metal Decking.

Section 05400 - Cold Formed Metal Framing.

Section 06100 - Rough Carpentry.

Section 07100 - Waterproofing.

Section 07260 - Vapor Barrier.

Section 07400 - Preformed Roofing and Cladding/Siding.

Section 07800 - Fireproofing.

Section 07840 - Thermal Barrier.

Section 07650 - Flexible Flashing.

Section 09110 - Metal Support Systems.

Section 09250 - Gypsum Board.

REFERENCES

** NOTE TO SPECIFIER ** Delete references from the list below that are not actually required by the text of the edited section.

American Society for Testing and Materials (ASTM):

ASTM C 518 - Standard Test Method for Steady-State Thermal Transmission Properties by Means of the Heat Flow Meter Apparatus.

ASTM D 1621 - Standard Test Method for Compressive Properties of Rigid Cellular Plastics.

ASTM D 1622 - Standard Test Method for Apparent Density of Rigid Cellular Plastics.

ASTM D 1623 - Standard Test Method for Tensile and Tensile Adhesion Properties of Rigid Cellular Plastics.

ASTM E 84 - Standard Test Method for Surface Burning Characteristics of Building Materials.

ASTM E 96 - Standard Test Methods for Water Vapor Transmission of Materials.

International Code Council – International Residential Code:

Section 103.7 - Alternate Materials and Methods.

2006 IRC Section R314 - Foam Plastic Insulation

2009, 2012 and 2015 IRC Section R316 - Foam Plastic Insulation.

Section 806.4 – 806.5 Unvented Attic Assemblies.

International Code Council – International Building Code:

Section 104.11 Alternative materials, design and methods of construction and equipment.

Section 2603 Foam Plastic Insulation.

SUBMITTALS

Submit under provisions of Section 01300.

Before commencing work, submit in accordance with local code.

Submit technical data sheets and samples as required by local code officials.

Submit the technical data sheet from the manufacturer showing the test results from the ASTM E84 (Surface Burning Characteristics).

Product Data: Manufacturer's data sheets on each product to be used, including:

Preparation instructions and recommendations.

Storage and handling requirements and recommendations.

Installation methods.

QUALITY ASSURANCE

Installer Qualifications:

Contractor performing work under this section shall be trained by DEMILEC® in the art of applying spray polyurethane foam insulation.

Provide current DEMILEC® Authorized Contractor Certificate.

** NOTE TO SPECIFIER ** Include a mock-up if the project size and/or quality warrant taking such a precaution.  The following is one example of how a mock-up on a large project might be specified.  When deciding on the extent of the mock-up, consider all the major different types of work on the project.

Mock-Up:  Provide a mock-up for evaluation of surface preparation techniques and application workmanship.

Finish areas designated by Architect.

Do not proceed with remaining work until installation is approved by Architect.

Rework mock-up area as required to produce acceptable work.

DELIVERY, STORAGE, AND HANDLING

Materials shall be delivered in manufacturer’s original containers clearly labelled with manufacturer’s name, product identification, safety information, net weight of contents and expiration date.

Material shall be stored in a safe manner and where the temperatures are in the limits specified by the material manufacturer.

Empty containers shall be removed from site on a daily basis.

Store and dispose of solvent-based materials, and materials used with solvent-based materials, in accordance with requirements of local authorities having jurisdiction.

PROJECT CONDITIONS

Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results.  Do not install products under environmental conditions outside manufacturer's absolute limits.

Ventilate insulation application area in accordance with the Spray Foam Coalition’s Guidance on best practices for the installation of Spray Polyurethane Foam.

Protect workers as recommended by the Spray Foam Coalition’s Guidance on best practices for the installation of Spray Polyurethane Foam.

Protect adjacent surfaces, windows, equipment and site areas from damage of overspray.

WARRANTY

Manufacturer’s Warranty:  DEMILEC® warrants spray-in-place urethane foam insulation, when installed by certified contractors using factory-trained applicators and applied in accordance with the Installation Instructions, will perform as stated in the Product Technical Data Sheet.

This warranty is in effect throughout the life of the building provided the original purchaser registers with the Warranty Department of the Manufacturer within thirty days of occupancy.

Manufacturer’s sole responsibility under this Limited Lifetime Warranty shall be to repair or replace any defective Product at the cost of the material only.

Manufacturer shall not be responsible for labor cost or any other costs whatsoever related to, or in connection with the removal or installation of either the original or replacement product.

PRODUCTS

MANUFACTURERS

Acceptable Manufacturer:  DEMILEC®; 3315 E. Division St., Arlington, TX 76011.  Toll Free Tel: (888) 224-1533.  Tel: (817) 640-4900.  Fax: (817) 633-2000.  Email: buildingscience@demilec.com.  Web: http://www.demilec.com

** NOTE TO SPECIFIER ** Delete two of the following three paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

Substitutions: Equivalent as judged by Architect

Contact DEMILEC®’s Building Science Department for product comparison data

817-640-4900

buildingscience@demilec.com

Requests for substitutions will be considered in accordance with provisions of Section 01600.

SPRAY FOAM INSULATION

** NOTE TO SPECIFIER ** HEATLOK® XT, a closed cell Spray Polyurethane Foam Insulation, has a unique ecological benefit that recycles plastic waste into a Rigid Spray Polyurethane Foam. This helps to more efficiently utilize the world’s non renewable resources. HEATLOK® XT can reduce excess waste and energy consumption in buildings by up to 50%. This closed-cell spray foam insulation offers both an air-barrier and vapor barrier in a single application and can be used in exterior or below grade applications. This material is approved by California Department of Consumer Affairs and is certified by GREENGUARD Gold for Office and Classrooms. Readily contributes to LEED certification.

** NOTE TO SPECIFIER ** There are two formulations for HEATLOK® XT, Summer and Winter, the chosen formulation is determined by the spray foam installer based on the environmental conditions of the application. While the physical properties are similar, there are some differences, a physical properties table is included herein to show a side-by-side comparison.

Delete if not required.

Spray Applied  Rigid Polyurethane Foam Insulation System: HEATLOK® HFO High Lift

Manufacturer: DEMILEC®, Arlington, TX

Product Approval:

Code Compliance Research Report, (CCRR) designed by Deer Ridge Consulting, Inc.

http://www.demilec.com/documents/Heatlok-HFO-High-Lift-CCRR.PDF

Approved for use in wall cavities, floor assemblies, ceiling assemblies or attics and crawl spaces in Type VB construction (IBC) and dwellings under the IRC.

Approved for use in building types I, II, III, IV, and V construction under IBC and dwellings for IRC.

Passed AC 377 Appendix X compliant NFPA 286.

Application Options:

Application with a prescriptive Thermal Barrier:

There is no thickness limit when installed in floors or ceilings behind 1/2 inch gypsum wall board or equivalent 15 minute thermal barrier in accordance with IBC 2603.4 or IRC R316.4.

Application without a Thermal Barrier

Up to 11-1/2 inches (292 mm) on the underside of the roof sheathing or in floor assemblies and 7-1/2 inches (191 mm) on vertical surfaces with:

A minimum of 12 dry mils of DC-315 Fireproof Paint

or

A minimum of 12 dry mils of Blazelok™ TBX

Attics and Crawlspaces: Passed AC 377 Appendix X compliant NFPA 286.

Up to 11-1/2 inches (292 mm) on the underside of the roof sheathing or in floor assemblies and 7-1/2 inches (191 mm) on vertical surfaces, the insulation may be left exposed without a thermal barrier, ignition barrier or intumescent coating

Use on Attic Floors

Up to 11-1/2 inches (190.5mm) between and over the joists in attic floors

Use as a Vapor Retarder: Class II vapor retarder @ < 1.0 perm, HEATLOK® HFO High Lift minimum thickness of 0.7 inches.

Physical Properties:

| Physical Property | Test Standard | HEATLOK® HFO High Lift |
| --- | --- | --- |
| R-Value/in @ 4 inch R-Value/in @ 1 inch | ASTM C 518 | 7.5 ft2 hoF/BTU 6.3 ft2 hoF/BTU |
| R-Value @ 6.5 inches R-Value @ 4 inches R-Value @ 2 inches | ASTM C 518 | 48 ft2 hoF/BTU 30 ft2 hoF/BTU 14 ft2 hoF/BTU |
| Core Density | ASTM D 1622 | 2.2 lb/ft3 |
| Water Vapor Permeance | ASTM E 96 | < 1 perm @ 0.7” |
| Air Permeance @ 75 Pa @ 1” | ASTM E 2178 | < 0.02 L/sm2 |
| Air Leakage @ 75 Pa @ 1” | ASTM E 283 | < 0.02 L/sm2 |
| Compressive Strength | ASTM D 1621 | 34.8 lb/in2 (240 kPa) |
| Tensile Strength | ASTM D 1623 | 101.3 lb/in2 (699 kPa) |
| Dimensional Stability | ASTM D 2126 | 11.4 (% volume change) @ 158o F (70oC) 97% R.H. |
| VOC Content | Greenguard Gold | PASS, Meets Criteria |
| Flame Spread | ASTM E84 | Class I 0-15 |
| Smoke Developed | ASTM E84 | Class I 350 – 400 |
| Recycled Content | Finished Foam Renewable & Recycled Content | 12% |
| Recycled Content | Polyol Renewable Content | 6% |
| Recycled Content | Polyol Recycled Content | 19% |
| Fungi Resistance | ASTM C 1338 | No Fungal Growth |
| Closed Cell Content | ASTM D 2856 | 91% |

ACCESSORY PRODUCTS

Water Based Intumescing coating:

Installation:

- Equipment used to apply the Water Based intumescent coating shall be an airless sprayer approved by the manufacturer.

Product: Blazelok™ TBX, Distributed by DEMILEC®, Manufactured by Thermal Product Research Corp. (TPR2).

Application: Follow manufacturer’s application recommendations.

Physical Properties:

Surface Burning Characteristics (ASTM E 84): Class I. Flame Spread Index <25, Smoke Developed Index <50.

Reference Heatlok® HFO High Lift Technical Data Sheet (TDS) for wet and dry mil thickness

Flash Point: None

Volatility/VOC: < 50 g/L

Non-toxic, drain safe, water based, non-fuming.

Color: White / Grey

Do not add tint

Wait minimum 24 hours prior to top coating with quality latex paint. Verify dryness with moisture meter. (Dry to touch, 2 to 3 hours depending on temperature and humidity).

Product: DC315 Intumescing Coating, Distributed by DEMILEC®, Manufactured by International Fireproof Technologies, Inc. (IFTI).

Application: Follow manufacturer’s application recommendations.

Physical Properties:

Surface Burning Characteristics (ASTM E 84): Class I. Flame Spread Index 0, Smoke Developed Index 25.

Reference Heatlok® HFO High Lift Technical Data Sheet (TDS) for wet and dry mil thickness

Flash Point: None

Volatility/VOC: 47 g/L

Non-toxic, drain safe, water based, non-fuming.

Color: Flat / Ice Grey

Do not add tint

Wait minimum 24 hours prior to top coating with quality latex paint. Verify dryness with moisture meter. (Drying Time: @ 77oF & 50% R.H. – To touch 1 – 2 hours, to recoat if required 2 – 4 hrs.).

EXECUTION

EXAMINATION

Do not begin installation until substrates have been properly prepared.

If substrate preparation is the responsibility of another installer, notify General Contractor, Architect or other point of contact of unsatisfactory preparation before proceeding.

Commencement of work outlined in this section shall be deemed as acceptance of existing work and conditions.

PREPARATION

Clean surfaces thoroughly prior to installation.

Apply only when surfaces and environmental conditions are within limits prescribed by the material manufacturer.

Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

INSTALLATION

Install in accordance with manufacturer's instructions.

Apply as recommended by manufacturer to thickness as indicated on drawings.

Equipment used to apply the foam insulation shall have fixed ratio positive displacement pumps approved by foam manufacturer.

PROTECTION

Protect installed products until completion of project.

Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION

# Footnotes

http://www.spraypolyurethane.org/GoodPractices

http://www.spraypolyurethane.org/WorkerProtection

http://www.demilec.com/documents/Tech-Library/Heatlok-HFO-High-Lift-Product-Application-Guide.pdf